## Slide 1: Automatic dV/dQ analysis and map of Neware data (Fixed upper cutoff DOD cells at 40°C)
Roby Gauthier, Jeff Dahn

## Slide 2: dV/dQ scanning on one cycle
The program do a scanning of all possible slippage and active electrode masses within a finite matrix.
Since we have 4 four parameter (+ slippage, - slippage, + mass, - mass), this correspond to a 4D matrix.
Here is a example of a 2D matrix scanning (the negative electrode parameters are fixed).
As seen in the gif, sometimes a part of the experimental data at large capacity is removed. This is due to the way the vector is build from interpolation. This will not impact the χ2 values later.
This is cycle 500 of cell ID 66824.

## Slide 3: χ2 results for a simple 2D matrix (sum between 20 and 170 mAh)

## Slide 4: The same cell ID and cycle number, but a 300 by 300 matrix.

## Slide 5: Matlab program vs by hand
Matlab program best:
-> m+ = 1.25 g
-> Slipp+ = -35 mAh
(Negative parameters fixed):
-> m- = 1.04 g
-> Slipp- = -3 mAh
By hand best:
-> m+ = 1.282 g
-> Slipp+ = -40.8 mAh
(Negative parameters fixed):
-> m- = 1.04 g
-> Slipp- = -3.2 mAh
It took 0.4 seconds to get this results using the Matlab program.
Results can improve with more precision, but take more computational time.

## Slide 6: Matlab program fitting vs VAWQuum program fitting
VAWQuum need two fitting to arrive to the solution (use gradient). The Matlab program map the entire space, unlike VAWQuum.
Having this map help use being confident that we didn’t find a local minimum and help us to have an concrete idea of the error.
66824 - Cycle 1

## Slide 7: What about many cycles?
Next, we will test our program on many cycles using a 2D matrix (Negative electrode mass fixed at 1 g and negative electrode slippage fixed at -3 mAh). 4D matrices are also possible within the program but they tend to add noise). We will show these 4D matrices results later.
The program find check up cycles if they are present and only scan some of them.
Overall, the program take around 1 minute per cell.
As input, the program need the following experimental data:
  Capacity data vs. cycle number (not the end capacity data!)
  Voltage vs. capacity data
  Current vs. time data
  Half-cell curves

## Slide 8: 2D matrices results

## Slide 9: 66824, Fixed upper cutoff, 100% DOD C/10, 40°C

## Slide 10: 66824, Fixed upper cutoff, 100% DOD C/10 , 40°C

## Slide 11: 66830, Fixed upper cutoff, 75% DOD C/10 , 40°C

## Slide 12: 66830, Fixed upper cutoff, 75% DOD C/10 , 40°C

## Slide 13: 66836, Fixed upper cutoff, 50% DOD C/10 , 40°C

## Slide 14: 66836, Fixed upper cutoff, 50% DOD C/10 , 40°C

## Slide 15: 66842, Fixed upper cutoff, 25% DOD C/10 , 40°C

## Slide 16: 66842, Fixed upper cutoff, 25% DOD C/10 , 40°C

## Slide 17: 2D matrices: Overall

## Slide 18: 4D matrices results
Longer waiting time: Around 15 minutes per cell instead of 1 minute, but better Positive electrode mass loss results?
All dV/dQ fits (4D scan) can be found at the end of this PPT.

## Slide 19: Results for fixed upper cutoff at 40°C and C/10

## Slide 20: Results for fixed upper cutoff at 40°C and C/10

## Slide 21: Results for fixed upper cutoff at 40°C and C/10

## Slide 22: Half-cell analysis (Neware data)
t = 22300 h
t = 21113 h
t = 20135 h
t = 22093 h
Numerical summary on the next page

## Slide 23: Numerical summary
 | 100% DOD | 75% DOD | 50% DOD | 25% DOD
Positive mass loss equivalent capacity (mAh) | 41 | 35 | 29 | 27
Lithium inventory loss [SEI] (mAh) | 73 | 72 | 66 | 59
Perceived capacity loss (mAh) | 37 | 40 | 36 | 29

## Slide 24: Conclusion and Future
Li inventory loss and positive mass loss trends can be seen versus DOD.
Test the program when the current is not constant (C/5, C/3 cells).
Test fixed lowercutoff cells.
Improve confidence that the program work as expected.
Improve tolerance to experimental noise?
Test cells that are not within the DOD matrix (C/10 check up).

## Slide 25: Cycling data: Fixed Upper cutoff 40°C (i.e. all 4.1 V)
Additional data

## Slide 26
~1170 cycles
~2370 cycles
~4120 cycles
~1580 cycles
~3330 cycles
~5960 cycles
~2090 cycles
~4470 cycles
~7410 cycles
~3610 cycles
~7350 cycles
~12650 cycles
a)
b)
c)
d)
e)
f)
g)
h)
i)
Figure 4

## Slide 27: 4D matrices: dV/dQ fits Orange: Experimental data Blue: Half-cell data
Additional data

## Slide 28: 66824 (100% DOD, C/10, fixed upper cutoff at 40°C)
Cycle = 2
Cycle = 236
Cycle = 1172
Cycle = 704

## Slide 29: 66830 (75% DOD, C/10, fixed upper cutoff at 40°C)
Cycle = 138
Cycle = 810
Cycle = 1482

## Slide 30: 66836 (50% DOD, C/10, fixed upper cutoff at 40°C)
Cycle = 185
Cycle = 1031
Cycle = 1877

## Slide 31: 66842 (25% DOD, C/10, fixed upper cutoff at 40°C)
Cycle = 354
Cycle = 2194
Cycle = 3574